Wetting Agents
Material	Liquid	Wetting Agent
Alkali Salts	Heptane	Twitchell Base
Alumina	Water	Sodium Hexameta Phosphate
Aluminum	Water	Alipal CO-436
Aluminum Oxide	Water	Sodium Hexameta Phosphate
Anthracite	Isopropyl Alcohol	-
Ash	Isopropyl Alcohol	-
Barium Carbonate	Isopropyl Alcohol	-
Barium Sulphate	Isopropyl Alcohol	-
Barium Titinate	Water	-
Brown Coal	Isopropyl Alcohol	-
Calcium Carbonate	Water	Sodium Hexameta Phosphate
Calcium Oxide	Isopropyl Alcohol	Sodium Hexameta Phosphate
Carbon Black	Isopropyl Alcohol	-
Cement	Isopropyl Alcohol	-
Charcoal	Isopropyl Alcohol	-
Chromium Oxide	Water	Triton X-100
Chromium Powder	Water	Triton X-100
Clay China	Water	Sodium Hexameta Phosphate
Coke	Isopropyl Alcohol	-
Copper Powder	Water	Alipal CO-436
Glass Powder	Water	Triton X-100
Hydrated Lime	Isopropyl Alcohol	-
Kaolin	Water	Sodium Hexameta Phophate
Lead	Water	Triton X-100
Lead oxide	Water	Aerosol OT
Magnetite	Water	Aerosol OT
Nickel	Water	Aerosol OS
Plaster	Isopropyl Alcohol	-
Red Lead	Water	-
Sand	Water	-
Silica	Water	Sodium Hexameta Phophate
Silicates	Water	Alipol CO-436
Steel Powder	Water	Triton X-100
Sugar	Heptane	Twitchell Base
Talcum	Water	Triton X-100
Tin	Isopropyl Alcohol	-
Titanium Dioxide	Water	Sodium Hexameta Phophate
Tricalcium Phosphate	Isopropyl Alcohol	-
Tungsten	Water	Triton X-100
Zinc	Water	Triton X-100
Zinc Oxide	Water	Aerosol OT
Zirconium Oxide	Water	Aerosol OT